## Slide 1: MAT224 for AL SPOKE
Ananth Sheshadri Kishore Pydimarry
Engineer Engineer (HRA-Assoc)
Mat 04, 2012

## Slide 2: Why MAT224
Material Fracture – LS-DYNA
MAT24
MAT224
Fracture is not based on Statr of Stress (SOS).
Material separation occurs even if state of stess is compression.
Underpredicts fracture even when its supposed to not to fail
Fracture surface can be developed based on different States of Stresses (SOS). Plastic strain to failure can be input as a function of
Tension SOS
Compression SOS
Shear SOS
Bi-axial SOS
Combined modes SOS
Fracture strain is dependent on mesh-size of the model through a regularization curve
Needs extensive material testing to collate data for each state of stress. SOS is defined by triaxiality and Lode parameter
No damage and No anisotropy considered
Similar to mat24 till necking

## Slide 3: Triaxiality and Lode Parameter
vm

## Slide 4: Specimens Cut from Wheel
1
2
3
4
5
Full Wheel
Approx final cut shapes @ Honda tossed to IMR for machining

## Slide 5: Different coupon test specimens
S1
S2
S3
T1
T2
Shear
A1
A2
A3
A4
Plane stress specimens
Plane strain specimens
Axi symmetric specimens

## Slide 6: Triaxiality State of Stress
(triaxiality)

## Slide 7: Typical Triaxiality and Lode values
Plane stress specimens
Axisymmetric
specimens
Plane Strain specimens
Shear
specimens
Compression
specimens

## Slide 8: Tensile testing and DIC
S1
Ep (spot value - surface) = 0.141
Ep (ratio method - inner) = 0.1511
Ep (MAT24 fit) = 0.16
Triaxiality and Lode based on MAT24 fit
Triax = -0.33
Lode = 1.0
used

## Slide 9: MAT24,224 PS –0.25mm hexmesh
S1
S2
S3
T1
T2
Shear

## Slide 10: MAT24,224 PS –0.25mm Tet-mesh

## Slide 11: MAT24 PS to Failure - Animation

## Slide 12: Developed MAT224 Fracture Surface

## Slide 13: MAT24 Failure

## Slide 14: MAT24 Based Regularization
0.224mm
Characteristic length of hex = volume/max surface area
0.450mm
0.899mm
1.500mm
2.868mm

## Slide 15: Regularization Curve
Sampling = 200 pts

## Slide 17
Component Testing

## Slide 18: 3-point Bending Results

## Slide 19: Compression Results